SHANDONG HENGCHI CRYSTALLITE NEW MATERIALS CO., LTD.

Driven by Technology, Committed to Quality

Company Address:
Southeast Corner of the Intersection of Chuangye Avenue and Changjiang Road, Zhangdian District, Zibo City, Shandong Province, China

Brief Introduction

Shandong HENGCHI CRYSTALLITE New Materials Co., Ltd. is a high-tech enterprise specializing in the production of Pesudo-boehmite (aluminum hydroxide gel) and various types of alumina-based catalyst carriers, utilizing a proprietary continuous decomposition process based on the carbonization method. The company has been certified under the ISO 9001 Quality Management System.

Products are manufactured using independently developed equipment for continuous decomposition via carbonization, ensuring stable quality, large specific surface area, and high activity. These products are primarily used in petroleum and coal chemical catalysts, high-end ceramics, semiconductors, electronics, and new energy sectors.Equipped with a comprehensive testing center and a professional R&D team, the company has, through years of development, passed evaluations by multiple materials research institutes and received widespread acclaim from customers. It is a certified supplier to Sinopec and its Catalyst Division.

Adhering to the principle of “Customer Needs Are Our Priority,” the company continuously enhances collaboration with leading universities and research institutes, striving for constant improvement and innovation. Tailored high-tech catalyst carriers with customized chemical compositions, physical and chemical properties, and shapes can be developed and manufactured upon request.

Shandong HENGCHI CRYSTALLITE sincerely welcomes collaboration from all sectors to create a better future together.

Corporate Philosophy

Technology as the Core, Quality as the Lifeline

Brand Identity

Technology · Quality · Responsibility

Corporate Culture

Rigor · Collaboration · Innovation

Core Values

Integrity as the Foundation
Customer-Centric Service
Pursuit of Innovation and Excellence
Commitment to Responsibility

Contact Us

General Manager: Mr. Deng Jianke – 18366302378
Sales Director: Mr. Liu Boshuai – 15698053326 (same number on WeChat)
Email: shield0de@126.com

General Macroporous Pesudo-boehmite

I. Product Properties

Pesudo-boehmite, also known as aluminum hydroxide gel, mono-hydrated alumina, or pseudo-monohydrate soft alumina, has the molecular formula Al₂O₃·H₂O. General Pesudo-boehmite refers to products with SiO₂, Na₂O, and Fe₂O₃ content equal to or greater than 0.005%. It is non-toxic, odorless, and tasteless, and appears as a fine powder.

II. Main Applications

This product series is characterized by stable quality and excellent physicochemical properties. It is widely used in various fields, including hydroprocessing catalysts for petroleum distillates, cracking catalysts (e.g., for gasoline hydro-upgrading), and catalysts in the refining and chemical industries.

| Product Name | Grade | CaO (%) | SiO₂ (%) | Fe₂O₃ (%) | Na₂O (%) | Specific Surface Area (m²/g) | Pore Volume (ml/g) | Dry Basis (%) | Gel Volume (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Silicon-Free Macroporous Pesudo-boehmite | CP-1 | ≤0.02 | ≤0.02 | ≤0.01 | ≤0.05 | 280-300 | ≥1.2 | 70±2 | 20-30 |
| Silicon-Free Macroporous Pesudo-boehmite | CP-2 | ≤0.02 | ≤0.02 | ≤0.01 | ≤0.05 | ≥300 | ≥1.1 | 70±2 | 5-20 |
| Silicon-Free Macroporous Pesudo-boehmite | CP-3 | ≤0.02 | ≤0.02 | ≤0.01 | ≤0.05 | ≥300 | ≥1.1 | 70±2 | 20-30 |
| Silicon-Free Macroporous Pesudo-boehmite | CP-4 | ≤0.02 | ≤0.02 | ≤0.01 | ≤0.05 | ≥300 | ≥1.1 | 70±2 | 30-40 |
| High-Silica Macroporous Pesudo-boehmite | CP-S-1 | ≤0.02 | 0-2 | ≤0.01 | ≤0.05 | ≥360 | ≥1.2 | 70±2 | - |
| High-Silica Macroporous Pesudo-boehmite | CP-S-2 | ≤0.02 | 2-4 | ≤0.01 | ≤0.05 | ≥380 | ≥1.2 | 70±2 | - |

Note: Specifications can be adjusted according to customer requirements.

High-Purity Macroporous Pesudo-boehmite

I. Product Properties

High-purity Pesudo-boehmite is produced by further purifying general Pesudo-boehmite. The contents of SiO₂, Na₂O, Fe₂O₃, and CaO are all ≤0.005% (50 ppm). Manufactured via a continuous carbonization decomposition process, this product contains no sulfate ions. It features a large pore volume and high specific surface area.

II. Main Applications

This product is primarily used as a catalyst carrier in the petroleum, chemical, and environmental protection industries. It is also applied in adsorption and separation processes, high-end ceramics, the electronics industry, polishing, papermaking and coatings, as well as new energy and battery sectors.

Technical Specifications – High-Purity Macroporous Pesudo-boehmite (HP) Series

| Product Name | Grade | CaO (ppm) | SiO₂ (ppm) / (%) | Fe₂O₃ (ppm) | Na₂O (ppm) | Specific Surface Area (m²/g) | Pore Volume (ml/g) | Dry Basis (%) | Gel Volume (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| High-Purity Macroporous Pesudo-boehmite | HP-1 | ≤50 | ≤50 | ≤50 | ≤50 | ≥300 | ≥1.1 | 70±2 | 20–30 |
| High-Purity Macroporous Pesudo-boehmite | HP-2 | ≤50 | ≤50 | ≤50 | ≤50 | ≥300 | ≥1.1 | 70±2 | 30–40 |
| High-Purity Macroporous Pesudo-boehmite | HP-3 | ≤50 | ≤50 | ≤50 | ≤50 | ≥300 | ≥1.1 | 70±2 | 40–55 |
| High-Silica High-Purity Macroporous Pesudo-boehmite | HP-S-1 | ≤50 | 0–2% | ≤50 | ≤50 | ≥360 | ≥1.1 | 70±2 | — |
| High-Silica High-Purity Macroporous Pesudo-boehmite | HP-S-2 | ≤50 | 2–4% | ≤50 | ≤50 | ≥380 | ≥1.2 | 70±2 | — |

Note: Specifications can be customized according to user requirements.

β - Al（OH）₃

I. Product Properties

β-Al(OH)₃ is a specialized aluminum-based material featuring a unique hexagonal layered structure. It is composed of aluminum-oxygen octahedral sheets (Al–O–Al) linked via hydrogen bonds to form a two-dimensional layered framework. The crystal phase purity exceeds 95%. The interlayer contains exchangeable Na⁺ and K⁺ ions, making it suitable for applications such as heavy metal adsorption and as a catalyst support. The product exhibits excellent thermal stability, making it well-suited for high-temperature catalytic reactions.

II. Main Applications

Hydrodesulfurization catalysts

Heavy metal removal

Lithium battery separator coatings

Structural ceramics

Bioceramics

Technical Specifications of β-Al(OH)₃

| Product Name | Grade | SiO₂ (%) | CaO (ppm) | Fe₂O₃ (%) | Na₂O (%) | Specific Surface Area (m²/g) | Bulk Density | D50 (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| β-Al(OH)₃ | BL-01 | 0.15 | ≤1500 | 0.06 | 0.3 | ≥350 | 0.88 | 20–30 |
| β-Al(OH)₃ | BL-02 | — | — | — | — | ≥460 | 0.67 | — |

LB Powder (Substitute for SB Powder)

I. Product Properties

LB Powder is an independently developed and processed product by the company, designed to serve as a substitute for imported SB Powder. It features excellent binding performance and rapid, clear acid solubility. The product has been tested and evaluated by several catalyst manufacturing companies.

II. Main Applications

Hydrotreating catalysts, environmental protection catalysts, lithium battery separator coatings, MLCC dielectric layers, structural ceramics, bioceramics, CVD coatings, photovoltaic silver paste, among others.

Technical Specifications of LB Powder

| Product Name | Grade | CaO (ppm) | SiO₂ (ppm) | Fe₂O₃ (ppm) | Na₂O (ppm) | Specific Surface Area (m²/g) | Pore Volume (ml/g) | Gel Volume (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LB Powder | LB-01 | ≤50 | ≤50 | ≤50 | ≤50 | 250-280 | 0.5-0.55 | ≥99 |

Microcrystalline Alumina

I. Product Characteristics

The α-phase microcrystalline alumina produced by the company is a high-performance alumina material characterized by a well-defined crystalline structure and unique physical properties. Its advantages include fine crystal size, high purity, controllable specific surface area, and stable physicochemical properties.

II. Main Applications

The α-phase microcrystalline alumina can be processed into a core material for ceramic substrates used in CED and IGBT module power chips, supporting circuit integration and heat dissipation. It is also suitable for manufacturing high-end insulators, ceramic capacitors, and microwave devices, meeting the dielectric constant requirements of 5G communication materials.

In lithium battery components, it serves as a coating material for separators to enhance battery safety or as a coating modifier for cathode materials to suppress interfacial side reactions. In advanced ceramics and refractory materials, it is used to produce special ceramic bearings, sealing rings, and cutting tools. Its high hardness and wear resistance make it applicable in mechanical and aerospace industries.

Additionally, it is used for grinding and polishing metals, glass, and stone, as well as in the production of ceramic joints and other medical ceramics.

Technical Specifications – α-Phase Microcrystalline Alumina

| Product Name | Grade | SiO₂ (ppm) | Fe₂O₃ (ppm) | Na₂O (ppm) | CaO (ppm) | MgO (ppm) | Calcination Temperature (℃) | α-Phase Content (%) | Particle Size (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Microcrystalline Alumina | MC-01 | ≤45 | ≤50 | ≤150 | ≤200 | 12 | 1230 | ≥96 | 0.5 |

Spherical Alumina Carrier

I. Product Applications

Catalyst Support: Enhances the dispersion, stability, and activity of catalysts. Widely used in petroleum refining, exhaust gas treatment, organic synthesis, and other fields.

Thermal Conductive Filler: Applied in thermal interface materials, thermally conductive engineering plastics, and aluminum-based copper-clad laminates to improve thermal conductivity.

II. Product Specifications

(Customizable according to user requirements)

| Appearance | Spherical |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Grades | AS-01，AS-02，AS-03 |  |  |  |  |  |
| Specification Item | Unit | Technical Requirement |  |  |  |  |
| Particle Size | mm | Φ1～2 | Φ2～3 | Φ3～4 | Φ4～6 | Φ15～25 |
| Loss on Ignition | % | ≤6.0 |  |  |  |  |
| Specific Surface Area | m2/g | 150-350 |  |  |  |  |
| Pore Volume | cm3/g | 0.5-0.9 |  |  |  |  |
| Bulk Density | g/cm3 | 0.4-0.75 |  |  |  |  |
| Crushing Strength | N/piece | ≥25 | ≥40 | ≥60 | ≥100 | ≥300 |
| Water Absorption | % | 60-150 |  |  |  |  |

| Appearance | Spherical |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Grades | AS-04，AS-05 |  |  |  |  |
| Specification Item | Unit | Technical Requirement |  |  |  |
| Particle Size | mm | Φ1～2 | Φ2～3 | Φ3～4 | Φ4～6 |
| Loss on Ignition | % | 0.5-5 |  |  |  |
| Specific Surface Area | m2/g | 150-350 |  |  |  |
| Pore Volume | cm3/g | 0.3-0.5 |  |  |  |
| Bulk Density | g/cm3 | 0.4-0.75 |  |  |  |
| Crushing Strength | N/piece | ≥25 | ≥40 | ≥60 | ≥100 |

Alumina Microspheres

I. Product Overview

This product appears as white or slightly reddish sand-like granules. It is non-toxic, odorless, and insoluble in water and organic solvents, but soluble in strong acids and alkalis. The AM series, developed with proprietary technology, features large pore volume (and diameter), high specific surface area, low attrition rate, and a concentrated particle size distribution.

II. Main Applications

As a new type of catalyst carrier, alumina microspheres offer numerous advantages, including fine particle size for accelerated reaction rates, ease of impregnation with rare earth metals and other catalytic components, and high catalytic activity. They are primarily used in fluidized bed catalysts for petrochemical processes, pharmaceutical catalysts, purification catalysts in the chemical industry, and as desiccants.

III. Technical Specifications

(Adjustable according to user requirements)

| Grade | SiO₂ (%) | Fe₂O₃ (%) | Na₂O (%) | Pore Volume (ml/g) | Specific Surface Area (m²/g) | Bulk Density (g/cm³) | Loss on Ignition (%) | Particle Size (mm) | Attrition (%) | Pore Diameter (nm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AM-01-C | ≤0.30 | ≤0.05 | 0.01～0.03 | 0.7～0.9 | 100～350 | 0.4～0.6 | ≤6.0 | 0.1～1 | ≤0.3 | 6-15 |
| AM-01-X | ≤0.30 |  |  | 0.5～0.7 | 100～350 | 0.4～0.6 |  |  |  |  |
| AM-02-C | ≥1 |  |  | 0.7～0.9 | 100～350 | 0.5～0.9 |  |  |  |  |
| AM-02-X | ≥1 |  |  | 0.5～0.7 | 100～350 | 0.5～0.9 |  |  |  |  |
| AM-03-C | ≤0.30 |  |  | 0.35～0.45 | 100～300 | 0.5～0.9 | ≤5.0 | 0.1～0.5 | ≤0.2 |  |
| AD-01 | ≤0.30 |  |  | 0.35～0.45 | 100～300 | 0.5～0.9 |  | 0.04～0.1 | ≤0.5 | / |

Note:
AD-01 is manufactured using spray-drying forming technology. It is primarily used as a catalyst in fluidized bed production, and also serves as a desiccant, adsorbent, carrier for melamine catalysts, and automotive exhaust catalysts.